GUIDE SPECIFICATIONS FOR ECHOSORB ACOUSTICAL PANELS

PART 1 GENERAL

1.1 SCOPE

1.1.1 The requirements of the instructions to Bidders, General Conditions, Supplementary General Conditions and Section apply to all work hereinafter specified.
1.1.2 This section shall include the furnishing of all tools, equipment and labor necessary to complete all acoustical panels work shown on drawings and/or herein specified.
1.1.3 Manufacturer shall furnish acoustical panels complete with hardware to provide complete installation. The acoustical panels hereinafter specified shall be installed by qualified factory trained craftsmen skilled in this trade.

1.2 RELATED WORK SPECIFIED ELSEWHERE

1.2.1 Section 03300 Cast-in-Place Concrete
1.2.2 Section 04200 Unit Masonry
1.2.3 Section 05100 Structural Metal Framing
1.2.4 Section 06100 Rough Carpentry
1.2.5 Section 06200 Finish Carpentry
1.2.6 Section 07920 Sealant and Caulking
1.2.7 Section 09250 Gypsum Board
1.2.8 Section 09300 Finish Ceilings
1.2.9 Section 09500 Acoustical Treatment
1.2.10 Section 09650 Finish Flooring
1.2.11 Section 09680 Carpet
1.2.12 Section 09900 Painting
1.2.13 Section 09950 Wall Coverings
1.2.14 Division 16 Electrical Work

1.3 REFERENCES

1.3.1 American Society for Testing and Materials (ASTM) Standard Test Method for Sound Absorption and Sound Absorption Coeffieients by the Reverberation Room Method:  ASTM C423-90a andE795-90a.

1.4 SUBMITTALS

1.4.1 One sample of each color material to be used on the project.
1.4.2 Copies of properly identified manufacturer's literature with proposed catalog numbers identified. Complete shop drawings showing elevations of units, locations in the buildings, conditions at openings with wall thickness and materials, typical and special details of construction, location and installation requirements for hardware shape and thickness of materials, joints and connections and material finishes.

1.5 PRODUCT DELIVERY, STORAGE AND HANDLING

1.5.1 Deliver materials to job site and protect unsealed materials from abrasions.
1.5.2 Identify each container with material name and identification number. Store materials under cover, protected from weather and construction activities. Safe storage of materials prior to installation is to be the responsibility of the general contractor.

1.6 ACCEPTABLE MANUFACTURERS
The following manufacturers are acceptable if the product bid meets the criteria outlined in the specifications and detailed on the drawings. All others must submit to the architect for approval, no less than 10 days prior to the bidding, sufficient information to show that their product will meet the intent of the specifications: PANELFOLD, INC.

PART 2 PRODUCTS

2.1 ACOUSTICAL WALL PANELS shall be EchoSorb as manufactured by Panelfold, Inc., Miami, Florida, U.S.A. and installed by an authorized representative of the manufacturer on walls prepared by others to EchoSorb requirements.

2.2 PANEL SIZES:  All standard acoustical wall panels shall be 24” (610mm) wide by 48” (1220mm) long.  Custom size panels shall be available from the manufacturer to specification in any size up to 48” 1220 wide by 96” (2464mm) long.

2.2 PANEL CONSTRUCTION: Panels shall be framed in heavy duty, extruded aluminum and backed with mdf (medium density fiberboard).  Panels shall be filled with 1” (25mm) thick Owens Corning 3 pcf (lbs per cubic foot)(.5kg/pcm-kg per cubic meter) density Fiberglas  unfaced insulation, and wrapped with acoustically transparent panel fabric.  The panel fabric shall be returned at the panel edges and stapled to the back of the panels with tailored corners.  Panels shall be 1 ¼” (32mm) thick overall.

2.3 PANEL FABRIC: Acoustically transparent 100% polyolefin fabric shall be Class A flame spread rated.  Colors shall be selected from manufacturer's standards (or as specified:__________.

2.4 N.R.C. ACOUSTICAL RATING: EchoSorb acoustical wall panels shall have been tested in an independent accredited acoustical laboratory and achieved a minimum N.R.C. .75 in accordance with ASTM C423-90a and E795-93.

2.5 HARDWARE: All mounting hardware suitable for applying the panels to the wall shall be supplied by the manufacturer.  There shall be no exposed fasteners or trim.

2.6 HANGING WEIGHT: Approximately 1.6 lbs./ft2(____kg/M2)

# PART 3 EXECUTION

3.1 EXECUTION
Before installation is commenced, inspect the opening. Surfaces shall be clean and dry. Concrete surfaces shall be free of excess mortar and lumps. Wood surfaces shall be well nailed and/or glued, nailed heads driven flush, and wood free of voids. Metal surfaces shall be free of grease, oil, dirt, rust, corrosion and welding slag, without sharp edges.

3.2 PREPARATION
Open containers and verify that all required parts are available and undamaged before disposing of containers. Arrange materials in proper sequence to conform to manufacturer's information and installation instructions.

3.3 INSTALLATION

Installer shall conform to the manufacturer's installation instruction sheets.

3.4 CLEANING

3.4.1 Clean all panel fabric surfaces to remove soil without using abrasive cleaners of solutions containing corrosive solvents.
3.4.2 Remove debris from worksite.

3.5 DEMONSTRATION

3.5.1 After all adjustments, lubrications and clean up, the installer shall demonstrate and instruct the proper operation, function and maintenance procedures for the panels.
3.5.2 Deliver all maintenance manuals to the owner.

NOTE:  The ASTM-84 procedure Class A flame spread and other test results referenced herein are to comparison purposes only and are not intended to reflect hazards presented by this or any other materials under actual fire conditions.

Panelfold is constantly developing its products and reserves the right to change specifications and materials without notice.